TITANIUM DIOXIDE

4010 GRANULAR

4010 is an ultra high purity, free flowing, non-dusting grade of titanium dioxide specifically engineered for optical clarity. 4010 is the consistent problem solver for batch processors experiencing dry component flow difficulties. It has specific applications in fiber optic glass systems, specialty glass, ceramics and other applications requiring high purity titanium dioxide and a low presence of transition (color-forming) elements.

Specification		       Typical Analysis

TiO2					 99.5% min			>99.7%

P					 0.05% max			<0.04%

S					 0.05% max			<0.04%

Fe					 50  ppm max		<35 ppm

Particle Size

Typical Dry Screen Analysis			Mesh		% Retained

+ 40		30 – 35%

+100		70 – 80%

+325		98% min

Packaging				1 MT Super Sacks