TITANIUM DIOXIDE

A-25

ANATASE PIGMENT

Applications:

A-25 is an anatase titanium dioxide pigment designed for easy dispersion in aqueous applications such as paper wet-end additions, paper coatings and in paints where chalking is permitted. A-25 is also suitable for use in ceramics, rubber, electro-ceramics, concrete curing compounds, and in finishes for leather and textiles.

Standards 			Typical Properties:

TiO2 Content				≥ 98%					98.9%

Particle Size, mean (d50)		0.24 – 0.30 µm			  0.28 µm

Retained on 325 Mesh		≤ 0.10%				  0.04%

Water Absorption			≤ 26 g/100g				25 g/100g

pH					6.5 – 8.0				  7.6

Volatile content @ 105° C		≤ 0.50%				  0.28%

Soluble matter in water		≤ 0.50%				  0.31%

Dispersibility in water		≥ 80%					81%

Color

Hunter L			≥ 98					98.3

CIE L*				Reference				98.7

GE/TAPPI Brightness		Reference				97.9

CIE Whiteness			Reference				97.9

Pigment Type:		Type 1 by ASTM D476

FDA:	A-25 is compliant with FDA regulations governing paper applications including 175.300, 176.170 and 176.180

CAS No.:	13463-67-7

Packaging:	50 lb. (22.7 kg) white repulpable paper bags with water soluble inks and adhesives

1 MT (2,204.6 lbs.) super sacks