TITANIUM DIOXIDE

A-300F

ANATASE

Applications:

A-300F anatase has a purity and particle size distribution specifically designed for use in synthetic fiber delustering and in plastic color concentrates.  It is suitable for use in polyamide, polyester, and cellulose-viscose fibers.

Standards 			Typical Properties:

TiO2 Content				≥ 98%					98.4%

Average Particle Size		≤ 0.3 µm				  0.28 µm

Retained on 325 Mesh		≤ .05%				  0.04%

Oil Absorption			≤ 26 g/100g				22 g/100g

pH					6.0 – 8.0				  7.6

Volatile content @ 105° C		Reference				  0.37%

Moisture				≤ 0.5%				  0.32%

Iron Oxide Content			≤ 0.007%				  0.006%

Color

Hunter L			≥ 97.5				            97.8

a			≤ 0.1					   0.1

b			≤ 0.5				              0.2

Resistivity in Water Extract		Reference				  30.8 Ω M

Specific Gravity			   3.9					    3.9

Pigment Type:		Type 1 by ASTM D476

CAS No.:	13463-67-7

Packaging:	25 kg (55.12 lb.) plastic bags stacked 40 bags/pallet.