TITANIUM DIOXIDE

R-1 RUTILE POWDER

R-1 is a non-pigment rutile titanium dioxide powder that exhibits relatively high surface area with a mean particle size of 3-5 microns. It is well suited for use in the production of electro-ceramics, specialty glass, fiberglass, engineered ceramics, coated welding rods, and titanium compounds.

Specification			Typical Analysis

TiO2					99.0% min			>99.5%

P  					 				<0.05%

S 					 				<0.05%

Fe 					 				<200 ppm

% Ignition Loss							<0.05%

Surface Area		Typical B.E.T. surface area is 1.4 m2/g

Particle Size			Typical mean particle size is 3-5 microns

Crystal Structure		Principally rutile (97% min)

Specific Gravity		4.2

Packaging			50 lb. PP bags with PE insert

(40 bags/pallet)

1 MT (2,205 lbs.) Super Sacks