TITANIUM DIOXIDE

R-501

RUTILE PIGMENT

Applications:

Solvent-based trade sales paint requiring limited weathering resistance

Road marking paint

Color masterbatches

Standards:

TiO2 Content                                				  ≥ 98.0%

Rutile Content                                                                 ≥ 97.0%

Retained on 325 Mesh                                                    ≤ 0.05%

Oil Absorption                                                                 ≤ 19 g/100g

pH                                                                                   ≥ 8.00

Volatile content @ 105° C                                               ≤ 0.4%

Tinctorial power (compared to standard)                         ≥ 100

Specific Gravity                                                                   4.2 g/cm3

Surface Treatments:	No Inorganics

Hydrophobic Organic

Classifications:		ISO 591		R1

ASTM D-476-84	Type II

CAS No.:	13463-67-7

Packaging:	25 kg (55.12 lb.) paper bags

500 kg (1102.3 lb.) super sacks

1000 kg (2,204.6 lb.) super sacks