TITANIUM DIOXIDE

R-602

RUTILE PIGMENT

Applications:		Water based paints

High quality paper

Standards:

TiO2 Content                                				  ≥ 93.0%

Rutile Content                                                                 ≥ 97.0%

Retained on 325 Mesh                                                    ≤ 0.05%

Water Absorption                                                            ≤ 22.0 g/100g

pH                                                                                      6.0 – 8.5

Volatile content @ 105° C                                               ≤ 0.7%

Resistivity                                                                        ≥ 4000 Ω/cm

Tinctorial power (compared to standard)                         ≥ 105

Specific Gravity                                                                   4.1 g/cm3

Surface Treatments:	Al2O3 and SiO2

Hydrophilic Organic

Classifications:		ISO 591		R2

ASTM D-476-84	Type II

CAS No.:	13463-67-7

Packaging:	25 kg (55.12 lb.) paper bags

500 kg (1102.3 lb.) super sacks

1000 kg (2,204.6 lb.) super sacks